Structure, electronic structure, dielectric and ferroelectric properties of lead free perovskite Ba1-xCaxTi0.9Zr0.1O3

G. Herrera-Pérez1, J. Canche-Tello2, M. E. Montero-Cabrera2, J. R. Plaisier3, D. Eichert3, A. Reyes-Rojas2, L. E. Fuentes-Cobas2,

1Catedrático CONACyT assigned to Centro de Investigación en Materiales Avanzados (CIMAV) S. C., Miguel de Cervantes 120, Chihuahua, Chih. 31136, Mexico

2Centro de Investigación en Materiales Avanzados (CIMAV) S. C., Miguel de Cervantes 120, Chihuahua, Chih. 31136, Mexico

3Elettra-Sincotrone Trieste S. C.p.A, Strada Statale 14, Km 163.5, Bassovizza, Trieste 34149, Italy

Email: guillermo.herrera@cimav.edu.mx

The electro-ceramic industry has focused their attention on replacing lead-based materials due to their toxic effects and unfavorable environment impact [1]. Barium titanate doped with calcium and zirconium is a well-known perovskite-type solid solution is a potential candidate that will cover this task in particular in the aeronautic industry [2]. Ba1-xCaxTi0.9Zr0.1O3 (where x = 0, 0.1 and 0.15) compositions are located near the called morphotropic phase boundary (MPB) that shows a coexistence of ferroelectric phases [1]. This work shows the relationship between the crystal and electronic structure with the dielectric and piezo-ferroelectric properties for these compositions prepared by the modified Pechini method [3]. The refinement (using the Rietveld method) of high-resolution X-ray diffraction (HR-XRD) patterns collected at the beamline 7.1 MCX (Elettra Sincrotrone) suggest the presence of single tetragonal phase over the obtained compositions. Figure 1a shows a two-dimensional grazing incidence X-ray diffraction pattern 2D-XRD collected for a Ba0.80Ca0.20Ti0.9Zr0.1O3 compound. The dielectric analysis indicates a relaxor behavior with a Curie temperature in a range of 100-120 oC. The ferroelectric evaluation complements the electrical characterization for these compositions [4]. Micro–X-ray absorption near edge spectroscopy (µ-XANES) was performed at the beamline 10.1L X-ray fluorescence (Elettra Sincrotrone) with the purpose to monitor possible changes of electronic structure profile at the Ti K-edge, due to the local distortions as Ca2+ increases (Figure 1b).

Figure 1. (a) 2D-GIXRD pattern collected at the 7.1 MCX beamline. (b) Normalized Ti K-edge spectra for the reference compound (BaTiO3) and other two representative compositions in order to monitor µ-XANES changes in the B1, B2, B3 and B4 features as the Ca concentration increases.

References

[1] Reyes-Montero A, Rubio-Marcos F, Pardo L, et al 2018 J. Mater. Chem. A 6 5419

[2] Jiménez K, Herrera-Pérez G, 2018 J. Mater. Sci. Engin. A 8 32-42

[3] Herrera-Pérez G, Morales D, Paraguay-Delgado F, et al 2016 J. Appl. Phys. 120 094303

[4] Herrera-Pérez G, Castillo-Sandoval I, Solís-Canto O, et al 2018 Mater. Research 21(2) e20170605